Product Name:  ZT3412

Appearance:  A silver black color, free flowing powder with a bland pearl luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     78-80             12001-26-2             77019

Pigment Black 7              20-22              1333-86-4              77266

D50

Particle Size Distribution: 80% within the range ＜15µm.        (By Malvern Mastersizer2000)

11.0±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           5.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       15-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)