Product Name:  ZT3625

Appearance:   An interference red color, free flowing powder with a bright pearl luster .

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     53-59             12001-26-2             77019

Titanium Oxide(TiO2)            41-47             13463-67-7             77891

Pigment Red 112                 <1              6535-46-2              12370

D50

Particle Size Distribution: 80% within the range10-60µm.        (By Malvern Mastersizer2000)

20.5±2.0

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       15-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)