Product Name:  ZT3425

Appearance:   A magic blue color, free flowing powder with a bright pearl luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     48-52             12001-26-2             77019

Titanium Oxide(TiO2)            48-52             13463-67-7             77891

Direct Sky Blue15               <1               2429-74-5              24400

D50

Particle Size Distribution: 90% within the range10-60µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       15-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)