Product Name:  Exterior Solar Orange9862WR

Appearance: A solar orange color, free flowing powder with a dazzling metal luster.

Ingredients and Composition

Chemical Name                %               CAS No.           CI No.

Synthetic Fluorphlogopite          40-44              12003-38-2

Iron(III) Oxide(Fe2O3)             52-56              1309-37-1           77491

Cerium Oxide (Ce2O3)                 <1                1345-13-7           77280

Polymer                    1-5

D50

Particle Size Distribution: 80% within（10-45）µm.        (By Malvern Mastersizer3000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     45-75 g oil/100g powder        GB 5211.15

Bulk Density:                       30-50 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)