Product Name:  Exterior Violet Cuckoo 96504WR

Appearance:  A free flowing off violet cuckoo powder with a bright metal luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite          50-53              12003-38-2

Iron(III) Oxide (Fe2O3)             42-48              1309-37-1               77491

Cerium Oxide (Ce2O3)                 <1                1345-13-7               77280

Polymer                          1-5

D50

Particle Size Distribution: 90% within the range10-60µm.         (By Malvern Mastersizer2000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     45-75 g oil/100g powder        GB 5211.15-88

Bulk Density:                       25-45 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)