Product Name:  Exterior Gold Pearl 9300WR

Appearance:  A bright gold color, free flowing powder with a bright highlights luster.

Ingredients and Composition

Chemical Name              %              CAS No.             CI No.

Mica                    52-61             12001-26-2             77019

Titanium Oxide (TiO2)           32-37             13463-67-7             77891

Iron(III) Oxide (Fe2O3)            1-5               1309-37-1              77491

Cerium Oxide (Ce2O3)               <1               1345-13-7              77280

Polymer                    1-5

D50

Particle Size Distribution: 90% within（8-40）µm.         (By Malvern Mastersizer3000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 5211.3

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       20-40 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)