Product Name:  Exterior Royal Gold Satin  9323WR

Appearance:  A gold color, free flowing powder with a bland luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                   43-51              12001-26-2             77019

Titanium Oxide (TiO2)            21-26              13463-67-7             77891

Iron(III) Oxide (Fe2O3)            21-26              1309-37-1              77491

Tin Oxide (SnO2)                  <1               18282-10-5             77861

Cerium Oxide (Ce2O3)                <1               1345-13-7              77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within (5-25)µm.         (By Malvern Mastersizer3000)

11.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     70-90 g oil/100g powder        GB 5211.15

Bulk Density:                       20-40 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)