Cosray Colored Coloron(Code:89IC1)

INCI Name:      Calcium Aluminum Borosilicate,Titanium Dioxide, Tin Oxide, Silica, Carmine

Chemical Composition:                                                                                                       Test method

Calcium Aluminum Borosilicate       50.0-60.0%                                                           CLRTM -51

TiO2                                                         15.0-25.0%                                                            CLRTM -48

SiO2                                                                                           25.0-35.0%                                                      CLRTM -48

SnO2                                                            ≤1.0%                                                        CLRTM -48

Carmine                                                  5.0-10.0%                                                      CLRTM -48

Appearance:                                          Lilac-Blue-Green                                                   CLRTM -52

Odor:                                                        Odorless                                                                CLRTM-53

Particle Size:                                          10-125μm                                                               CLRTM -42

pH-Value(10% Aqueous Suspension): 4.0-9.0                                                                    CLRTM -45

Oil Absorption:                                      50-90g/100g                                                          CLRTM -46

Density                                                    2.3-2.8g/cm3                                                          CLRTM -47

Microbiology:                                         <100 cfu/g                                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                      CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Cd                                                              <5ppm

Cr                                                              <100ppm

Ni                                                              <200ppm