Product Name:  Crystal Mica Iron Metal Luster Series SW6524

Appearance:    A wine red color, free flowing powder with a bright metal luster.

Ingredients and Composition

Chemical Name                 %               CAS No.            CI No.

Synthetic Fluorphlogopite           50-58             12003-38-2

Iron(III) Oxide(Fe2O3)              42-50             1309-37-1             77491

D50

Particle Size Distribution: 80% within the range 10-30µm.        (By Malvern Mastersizer2000)

14±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -7.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     45-75 g oil/100g powder        GB 5211.15-88

Bulk Density:                       25-45 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)