Product Name:  SW6570

Appearance:  A free flowing bronze powder with a bronze reflection with luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Mica              82-92            12003-38-2

Iron(III) Oxide(Fe2O3)           8-18             1309-37-1             77891

Particle Size Distribution: 80% within the range40-200µm.        (By Malvern Mastersizer2000)

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-8.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     50-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       10-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)