Product Name:  Warm satin gold   SW6326

Appearance:  Platinum Gold.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                    25-35              12001-26-2             77019

Titanium Oxide (TiO2)             52-58              13463-67-7             77891

Tin oxide (SnO2) 	≤1               18282-10-5             77861

Iron Oxide (Fe2O3)                     12-14              1309-37-1              77491

D50

Particle Size Distribution: 90% within the range5-25µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     50-70g oil/100g powder        GB 5211.15-88

Bulk Density:                       38-45g/100cm3              GB/T 23771-2009

Density                            3.1-3.6g / cm3 (water=1)