Product Name:  Super Flash Green Gold   SW6375

Appearance:  Platinum Gold.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite        56-71              12003-38-2             77019

Titanium Oxide (TiO2)           24-35              13463-67-7             77891

Tin dioxide (SnO2)              ≤1               18282-10-5             77861

Iron Oxide (Fe2O3)                  5-8                1309-37-1              77491

Polymer                 1-5

D50

Particle Size Distribution: 90% within the range70-500µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     80-120g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-45g/100cm3              GB/T 23771-2009

Density                            2.35-2.60g / cm3 (water=1)