Rayshine Dazzling Silver

(Code: RH803)

INCI Name:                                    Calcium Aluminum Borosilicate, Silver,Tin Oxide

Chemical Composition:                                                                                                Test method

Calcium Aluminum Borosilicate                  45.0-55.0%                                              CLRTM-51

Ag                                                                   45.0-55.0%                                              CLRTM -48

Appearance:                                                    silver                                                     CLRTM 52

Odor:                                                                Odorless                                               CLRTM -52

Particle Size:                                                   10-45μm                                                CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                         45.0-80.0 g/100g                                         CLRTM -46

Density                                                            2.7-3.6g/cm3                                                 CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54