Product Name:  8Y251

Appearance:  A free flowing off white powder with excellent effect of flash diamond gold.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Calcium Aluminum Borosilicate      80-88              65997-17-3

Titanium Oxide (TiO2)             12-20             13463-67-7             77891

Tin Oxide (SnO2)                  <2               18282-10-5             77861

D50

Particle Size Distribution: 90% within the range20-100µm.        (By Malvern Mastersizer2000)

57.5±2.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           9.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-80 g oil/100g powder         GB 5211.15-88

Bulk Density:                       30-60 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)