Cosray Crystal Royal Blue

(Code: 64402B)

INCI Name:Synthetic fluorphlogopite, Titanium Dioxide, Ferric Ammonium Ferrocyanide,

Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                 34.0-59.0%                                           CLRTM-51

TiO2 (Rutile)                                                  42.0-50.0%                                            CLRTM -48

Ferric Ferrocyanide                                     5.0-15.0%                                              CLRTM -48

SnO2                                                               ≤1.0%                                                CLRTM -48

Appearance:                                                   Blue Powder                                           CLRTM -52

Odor:                                                                   Odorless                                             CLRTM -53

Particle Size:                                                    10-60μm                                               CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             45.0-75.0g/100g                                       CLRTM -46

Density                                                               2.9-3.7g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm