Cosray Crystal Citrine

(Code: 6411Y)

INCI Name:                  Synthetic fluorphlogopite, Titanium Dioxide, Yellow 5 Lake, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                  64.0-83.0%                                           CLRTM-51

TiO2 (Rutile)                                                      12.0-20.0%                                           CLRTM -48

FD&C Yellow 5 Al Lake                                  5.0-15.0%                                             CLRTM -48

SnO2                                                                   ≤1.0%                                                 CLRTM -48

Appearance:                                                Yellow Powder                                          CLRTM -52

Odor:                                                                   Odorless                                             CLRTM -53

Particle Size:                                                    10-125μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                  CLRTM-45

Oil Absorption:                                             70.0-110.0g/100g                                    CLRTM -46

Density                                                               2.5-3.5g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm