Cosray Black

(Code: 64106SF)

INCI Name:  Synthetic fluorphlogopite, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                               25.0-35.0%                                               CLRTM-51

Black Iron Oxide                                          65.0-75.0%                                              CLRTM -48

Appearance:                                                      Black                                                   CLRTM -52

Odor:                                                                 Odorless                                               CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             65.0-100.0g/100g                                    CLRTM -46

Density                                                               2.8-3.5g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm