SPECIFICATION

Cosray Red Blue (Code: 4425BR)

| INCI Name: |  | Mica, Titanium Dioxide, Tin Oxide, Blue 1 Lake |  |
| --- | --- | --- | --- |
| Chemical Composition: |  |  | Test method |
| Mica |  | 37.0-56.0% | CLRTM-51 |
| TiO2 (Rutile) |  | 39.0-47.0% | CLRTM -48 |
| FD&C Blue 1 Al Lake |  | 5.0-15.0% | CLRTM -48 |
| SnO2 |  | ≤ 1.0% | CLRTM -48 |
| Appearance: | Blue Powder with Interference Red |  | CLRTM -52 |
| Odor: |  | Odorless | CLRTM -53 |
| Particle Size: |  | 10-60¦m | CLRTM -42 |
| pH-Value(10% Aqueous Suspension): |  | 4.0-11.0 | CLRTM-45 |
| Oil Absorption: |  | 60.0-100.0g/100g | CLRTM -46 |
| Density |  | 2.1-2.9g/cm3 | CLRTM -47 |
| Microbiology: |  | <100 cfu/g | CLRTM -54 |
|  |  | No gram negative |  |
| Heavy Metals: |  |  | CLRTM -55 |
| As |  | <3ppm |  |
| Pb |  | <10ppm |  |
| Hg |  | <1ppm |  |
| Sb |  | <2ppm |  |
| Cd |  | <1ppm |  |
| Zn |  | <50ppm |  |

ZZhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com