Cosray Super Green

(Code: 6205C)

INCI Name:    Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                             27.0-38.0 %                                               CLRTM-51

TiO2 (Rutile)                                               62.0-72.0%                                                 CLRTM -48

SnO2                                                              ≤1.0%                                                    CLRTM -48

Appearance:                                               Interference Green                                    CLRTM 52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   10-60μm                                                CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                           45-90g/100g                                              CLRTM -46

Density                                                             2.6-3.6g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm

Cr                                                                      <100ppm

Ni                                                                      <200ppm