Cosray Crystal Super White

(Code: 6106C)

INCI Name:                                  Synthetic Fluorphlogopite, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                           70.0-80.0%                                                  CLRTM-51

TiO2                                                          20.0-30.0%                                                    CLRTM -48

SnO2                                                          ≤1.0%                                                           CLRTM -48

Appearance:                                            Super White                                                  CLRTM 52

Odor:                                                            Odorless                                                    CLRTM -52

Particle Size:                                                10-60μm                                                   CLRTM -42

pH-Value(10% Aqueous Suspension):          4.0-11.0                                                  CLRTM -45

Oil Absorption:                                        50.0-90.0g/100g                                           CLRTM -46

Density ：                                                        2.7-3.2g/cm3                                          CLRTM -47

Microbiology:                                              <100 cfu/g                                                 CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm