Cosray Sparkle Wine Red

(Code:5053C)

INCI Name:                                          Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                             60.0-73.0%                                                  CLRTM-51

Fe2O3                                                          27.0-40.0%                                                 CLRTM -48

Appearance:                                         Sparkle Wine Red                                            CLRTM -52

Odor:                                                            Odorless                                                    CLRTM -53

Particle Size:                                               10-125μm                                                   CLRTM -42

Median size(D50):                                    40.0-80.0μm

pH-Value(10% Aqueous Suspension):        4.0-11.0                                                    CLRTM -45

Oil Absorption:                                     50.0-110.0g/100g                                             CLRTM -46

Density                                                                2.7-3.6g/cm3                                              CLRTM -47

Microbiology:                                           <100 cfu/g

No gram negative                                           CLRTM -54

Heavy Metals:                                                                                                                CLRTM -55

As                                                                  <3ppm

Pb                                                                  <10ppm

Hg                                                                 <1ppm

Ba                                                                  <50ppm

Cd                                                                  <5ppm

Cr                                                                  <100ppm

Cu                                                                 <50ppm

Ni                                                                  <200ppm

Zn                                                                 <100ppm