Cosray Sparkle Bronze

(Code: 5051C)

INCI Name:                                                  Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                     68.0-80.0%                                         CLRTM -51

Fe2O3                                                                  20.0-32.0%                                         CLRTM -48

Appearance:                                                  Sparkle Bronze                                       CLRTM -52

Odor:                                                                    Odorless                                            CLRTM -53

Particle Size:                                                       10-125μm                                           CLRTM -42

pH-Value(10% Aqueous Suspension):                4.0-11.0                                            CLRTM -45

Oil Absorption:                                              50.0-110.0g/100g                                    CLRTM -46

Density                                                                2.7-3.6g/cm3                                              CLRTM -47

Microbiology:                                                    <100 cfu/g

No gram negative                                   CLRTM -54

Heavy Metals:                                                                                                                CLRTM -55

As                                                                           <3ppm

Pb                                                                           <10ppm

Hg                                                                           <1ppm

Ba                                                                           <50ppm

Cd                                                                           <5ppm

Cr                                                                           <100ppm

Cu                                                                          <50ppm

Ni                                                                           <200ppm

Zn                                                                          <100ppm