Cosray Glitter Bronze

(Code:5031C)

INCI Name:                                                    Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                      65.0-82.0%                                         CLRTM-51

Fe2O3                                                                   18.0-35.0%                                        CLRTM -48

Appearance:                                                    Glitter Bronze                                        CLRTM -52

Odor:                                                                     Odorless                                           CLRTM -53

Particle Size:                                                         10-95μm                                           CLRTM -42

Median size(D50):                                              33-63μm

pH-Value(10% Aqueous Suspension):               4.0-11.0                                             CLRTM -45

Oil Absorption:                                              50.0-110.0g/100g                                   CLRTM -46

Density                                                                2.7-3.5g/cm3                                              CLRTM -47

Microbiology:                                                    <100 cfu/g                                           CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                            <3ppm

Pb                                                                           <10ppm

Hg                                                                           <1ppm

Ba                                                                           <50ppm

Cd                                                                           <5ppm

Cr                                                                           <100ppm

Cu                                                                          <50ppm

Ni                                                                           <200ppm

Zn                                                                          <100ppm