Cosray Coffee

(Code:5006C)

INCI Name:                                                    Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                      35.0-47.0%                                         CLRTM-51

Fe2O3                                                                   53.0-65.0%                                        CLRTM -48

Appearance:                                                         Coffee                                               CLRTM -52

Odor                                                                      Odorless                                           CLRTM -53

Particle Size                                                          10-60μm                                           CLRTM -42

Median size(D50):                                              16.0-28.0μm

pH-Value(10% Aqueous Suspension)                4.0-11.0                                             CLRTM -45

Oil Absorption                                               30.0-80.0g/100g                                      CLRTM -46

Density                                                                 3.1-3.9g/cm3                                              CLRTM -47

Microbiology:                                                    <100 cfu/g                                           CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                            <3ppm

Pb                                                                           <10ppm

Hg                                                                          <1ppm

Ba                                                                        <50ppm

Cd                                                                         <5ppm

Cr                                                                          <100ppm

Cu                                                                         <50ppm

Ni                                                                          <200ppm

Zn                                                                         <100ppm