Cosray Green Gold

(Code: 3008C)

INCI Name:                                     Mica,Titanium Dioxide,Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                           35.0-55.0%                                                    CLRTM-51

TiO2                                                          30.0-45.0%                                                    CLRTM -48

Fe2O3                                                       4.0-15.0%                                                      CLRTM -48

Appearance:                                              Golden                                                         CLRTM -52

Odor:                                                         Odorless                                                       CLRTM -53

Particle Size:                                            10-60μm                                                        CLRTM -42

pH-Value(10% Aqueous Suspension):   4.0-11.0                                                        CLRTM -45

Oil Absorption:                                       50.0-100.0g/100g                                          CLRTM -46

Density                                                         2.7-3.6g/cm3                                                    CLRTM -47

Microbiology:                                          <100 cfu/g                                                     CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Sb                                                              <2ppm

Ba                                                             <50ppm

Cd                                                             <1ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <50ppm