Cosray Super Gold

(Code: 2031C)

INCI Name:                                             Mica, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                 62.0-73.0%                                             CLRTM-51

TiO2 (Rutile)                                                    27.0-37.0%                                             CLRTM -48

SnO2                                                                      ≤1.0%                                             CLRTM -48

Appearance:                                                 Interference Gold                                    CLRTM 52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   20-80μm                                                CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                          50.0-80.0g/100g                                         CLRTM -46

Density                                                            2.8-3.4g/cm3                                                 CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm