Cosray Micro White

(Code: 1008C)

INCI Name:                                            Mica, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                                       Test method

Mica                                                                  47.0-59.0%                                                   CLRTM -51

TiO2 (Rutile)                                                    41.0-52.0%                                                   CLRTM -48

SnO2                                                                  ≤1.0%                                                        CLRTM -48

Appearance:                                                   Silver white                                                   CLRTM -52

Odor:                                                               Odorless                                                       CLRTM - 53

Particle Size:                                                       <15μm                                                      CLRTM - 42

pH-Value(10% Aqueous Suspension):              4.0-11.0                                                     CLRTM-45

Oil Absorption:                                             50.0-90.0g/100g                                             CLRTM -46

Density                                                               2.9-3.6g/cm3                                               CLRTM -47

Microbiology:                                                   <100 cfu/g                                                   CLRTM 54

No gram negative

Heavy Metals:                                                                                                                      CLRTM -55

As                                                                         <3ppm

Pb                                                                        <10ppm

Hg                                                                       <1ppm

Sb                                                                        <2ppm

Cd                                                                       <1ppm

Zn                                                                       <50ppm