Product Name:  Golden palace   SW6305

Appearance:  Golden powder.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite          30-40              12003-38-2             77019

Titanium Oxide (TiO2)            48-54              13463-67-7             77891

Iron Oxide（Fe2O3）              ≤1               1309-37-1              77491

Diiron Trioxide（Fe2O3）          12-15             18282-10-5             77861

Polymer                  1-5

D50

Particle Size Distribution: 90% within the range10-60µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-80g oil/100g powder        GB 5211.15-88

Bulk Density:                       35-43g/100cm3              GB/T 23771-2009

Density                            3.1-3.6g / cm3 (water=1)