Product Name:  Multi-Colour Series 1173S

Appearance:  A free flowing off white powder with a brown /red/violet multicolor effect.

Ingredients and Composition

Chemical Name              %               CAS No.               CI No.

Synthetic Fluorphlogopite          40-50              12003-38-2

Titanium Oxide(TiO2)            3-5                13463-67-7               77891

Iron(III) Oxide(Fe2O3)           15-20               1309-37-1                77491

Silicon Oxide (SiO2)           25-35                 7631-86-9

D50

Particle Size Distribution: 80% within the range10-45 µm.         (By Malvern Mastersizer2000)

25.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           5.0 -8.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)