Product Name:  Multi-Colour Series 1345A

Appearance:  A free flowing off white powder with a violet/blue/green multicolor sparkle effect.

Ingredients and Composition

Chemical Name               %               CAS No.               CI No.

Calcium Aluminum Borosilicate         85-93              65997-17-3

Titanium Oxide(TiO2)             5-13               13463-67-7               77891

Tin Oxide (SnO2)                  <2               18282-10-5                77861

D50

Particle Size Distribution: 80% within the range50-200 µm.        (By Malvern Mastersizer2000)

105±5.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -11.0                   ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     50-80 g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)