Coloron Pigment

(Code:62345MS)

INCI Name:              Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide, Silica, Iron Oxide

Chemical Composition:                                                                                                      Test method

Synthetic mica                                           45.0-69.0%                                                     CLRTM -51

TiO2                                                                10.0-17.0%                                                     CLRTM -48

SnO2                                                              ≤1.0%                                                            CLRTM -48

SiO2                                                                                               10.0-20.0%                                                  CLRTM -48

Fe2O3                                                          10.0-17.0%                                                   CLRTM -48

Appearance:                                                 Lilac-Blue-Green                                           CLRTM -52

Odor:                                                            Odorless                                                          CLRTM-53

Particle Size:                                                20-80μm                                                          CLRTM -42

pH-Value(10% Aqueous Suspension):       4.0-11.0                                                           CLRTM -45

Oil Absorption:                                           30-70g/100g                                                    CLRTM -46

Density                                                         2.8-3.6g/cm3                                                   CLRTM -47

Microbiology:                                             <100 cfu/g                                                       CLRTM -54