Coloron Pigment

(Code:62734MT)

INCI Name:            Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide, Silica, Iron Oxide

Chemical Composition:                                                                                                       Test method

Synthetic mica                                          52.0-74.0%                                                      CLRTM -51

TiO2                                                               10.0-17.0%                                                      CLRTM -48

SnO2                                                               ≤1.0%                                                            CLRTM -48

SiO2                                                                                              10.0-20.0%                                                    CLRTM -48

Fe2O3                                                          6.0-1020%                                                     CLRTM -48

Appearance:                                                 Orange-Lilac-Blue                                          CLRTM -52

Odor:                                                            Odorless                                                           CLRTM-53

Particle Size:                                                20-80μm                                                           CLRTM -42

pH-Value(10% Aqueous Suspension):       4.0-11.0                                                            CLRTM -45

Oil Absorption:                                           30-70g/100g                                                     CLRTM -46

Density                                                         2.8-3.6g/cm3                                                     CLRTM -47

Microbiology:                                              <100 cfu/g                                                        CLRTM -54