Cosray Colored Coloron 63IY1-X

INCI Name:   Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide, Silica,  Red 40 Al Lake , Yellow 5 Al  Lake

Chemical Composition:                                                                                                      Test method

Synthetic fluorphlogopite                          43.0-64.0%                                                      CLRTM -51

TiO2                                                                14.0-18.0%                                                     CLRTM -48

SnO2                                                              ≤1.0%                                                            CLRTM -48

SiO2                                                              11.0-21.0%                                                    CLRTM -48

FD＆C Yellow 5 Al Lake                             10.0-14.0%                                                       CLRTM -48

FD＆C Red 40 Al Lake                                 1.0-3.0%                                                          CLRTM -48

Appearance:                                             Lilac-Yellow Green                                             CLRTM -52

Odor:                                                            Odorless                                                          CLRTM-53

Particle Size:                                                20-80 μm                                                         CLRTM -42

pH-Value(10% Aqueous Suspension):       4.0-9.0                                                            CLRTM -45

Oil Absorption:                                           50-90g/100g                                                    CLRTM -46

Density                                                         2.5-3.6g/cm3                                                   CLRTM -47

Microbiology:                                             <100 cfu/g                                                       CLRTM -54

No gram negative

Heavy Metals:                                                                                                                     CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Cd                                                              <5ppm

Cr                                                              <100ppm

Ni                                                              <200ppm