Product Name:  Colour Series ZT3404

Appearance:  A lilac color, free flowing powder with a bright pearl luster

Ingredients and Composition

Chemical Name               %               CAS No.          CI No.

Mica                    70-78             12001-26-2          77019

Titanium Oxide(TiO2)             22-29             13463-67-7          77891

Direct Blue 86                 <1               1330-38-7           74180

Direct Red 80                  <1               2610-10-8           35780

D50

Particle Size Distribution: 80% within the range 10-60 µm.       (By Malvern Mastersizer2000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)