Cosray Yellow Green

(Code: 64501GY)

INCI Name: Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide, Chromium Oxide Green

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                  42.0-61.0%                                           CLRTM-51

TiO2 (Rutile)                                                      34.0-42.0%                                           CLRTM -48

Chromium Oxide Green                                   5.0-15.0%                                             CLRTM -48

SnO2                                                                      ≤1%                                                CLRTM -48

Appearance:                          Green Powder with Interference Yellow                       CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             70.0-110.0g/100g                                    CLRTM -46

Density                                                               2.9-3.6g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm