Cosray Rose Pink

(Code: 4308VC)

INCI Name:   Mica, Titanium Dioxide,Carmine, Tin Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                 38.0-54.0%                                           CLRTM-51

TiO2 (Rutile)                                                    44.0-53.0%                                           CLRTM-48

Carmine                                                            2.0-8.0%                                              CLRTM-48

SnO2                                                                  ≤1.0%                                               CLRTM -48

Appearance:                                                    Rose Pink                                             CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             45.0-75.0g/100g                                       CLRTM -46

Density                                                               2.9-3.7g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <10ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm

Cr                                                                      <100ppm

Ni                                                                     <200ppm